## Slide 1: Mechanical properties of elastin
Measured with ligament after having removed the collagen.
E= 200-400 kPa;
very narrow hysteresis loop;
ductility up to 130%;
negligible relaxation
Neck ligament
Neck ligament
loading
unloading
time (minutes)
stretch ratio

## Slide 2: Mechanical properties of collagen
Measured with a tendon – created of a nearly pure collagen.
E= 100-2000 MPa;
narrow hysteresis loop;
ductility 4 - 10%;
Strength 90-130 MPa;
relaxation more pronounced
Tendon
Tendon
stretch ratio
time (minutes)

## Slide 3: Mechanical properties of smooth muscle tissue
time (minutes)
stretch ratio
Smooth muscle tissue of intestine
Smooth muscle tissue of intestine
Measured with smooth muscle tissue of intestine in a passive (relaxed) state.
E= 15-25 kPa;
broad hysteresis loop;
very prononounced relaxation

## Slide 4: Influence of smooth muscle excitation on the arterial wall stiffness (canine carotid artery)
Inner pressure
Change of artery radius
Smooth muscle cells relaxed
Smooth muscle cells excited