## Slide 1: ASSESSMENT OF AMPLITUDE FACTORS OF ASYMPTOTIC EXPANSION AT CRACK TIP IN FLEXOELECTRIC SOLID UNDER MODE I LOADINGS
Profant T., Sládek J., Sládek V., Kotoul M.
Slovak Academy of Sciences, Slovak Republic
Brno University of Technology, Czech Republic

## Slide 2
Motivation
Is there a way how to determine the asymptotic solution of the fracture problem in the flexoelectric solid from the characteristics of LEFM?
If yes, what method and assumptions should be used to achieve adequate results, and which are their limitations?
Outline
  The flexoelectricity in solids
  The outer and inner asymptotic solution in the flexoelectric solid
  The singular matched asymptotic expansion method
  Numerical results

## Slide 3
The flexoelectricity in solids
Wang et. al., Progress in Materials Science, 106, 2019
The flexoelectric effect is the consequence of the coupling of the strain gradients and the electric polarization in dielectric materials.
The flexoelectric effect is the size dependent material property.
The strain gradients usually occur near the crack tip and therefore it is relevant to suppose that the crack formation and propagation is affected by the flexoelectricity in the dielectric materials.

## Slide 4
The flexoelectricity in solids
Governing equations
Constitutive equations
Boundary conditions
material length scale parameter
flexoelectric parameters
double stress

## Slide 5
classical elasticity
flexo
nonlocal
local
The flexoelectricity in solids

## Slide 6
The outer and inner asymptotic solution in the flexoelectric solid
FEM study: ,
inner solution
outer solution
flexo FEM: Sládek & Sládek et. al., International Journal of Solids and Structures, 2021
SGET FEM: Kotoul et . al., Fatigue & Fracture of Engineering Materials & Structures, 2020

## Slide 7
, , , , , , ,
symmetry
isolated and traction free crack faces
INPUT
4th-order differential equations
, ,
, ,
OUTPUT
crack
outer asymptotic
solution
inner asymptotic solution
Analytical solution:
Mao & Purohit, Journal of the Mechanics and Physics of Solids, 2015
The outer and inner asymptotic solution in the flexoelectric solid

## Slide 8
The outer and inner asymptotic solution in the flexoelectric solid
Outer solution:
Inner solution:
gauge

## Slide 9
The singular matched asymptotic expansion method
out
in
for
and for

## Slide 10
The singular matched asymptotic expansion method

## Slide 11
The singular matched asymptotic expansion method
Mao & Purohit, Journal of the Mechanics and Physics of Solids, 2015

## Slide 12
Numerical results
The influence of the flecoelectricity and Poisson ratio on the parameter
,

## Slide 13
Numerical results
The influence of the component on the inner asymptotic solution
, , , , 0.2

## Slide 14
Numerical results
The crack opening displacement
, ,

## Slide 15
Numerical results
The Cauchy stress in front of the crack tip
, ,

## Slide 16
Numerical results
The electric potential in front of the crack tip
, , ,

## Slide 17
The authors acknowledge the supports by the Slovak Science and Technology Assistance Agency registered under number APVV-18-0004, VEGA-2/0061/20
Thank you for your attention