## Slide 1: Odhad součinitelů asymptotického rozvoje trhliny ve flexoelektrickém materiálu při zatížení modem I a II
Profant T., Sládek J., Sládek V., Kotoul M.
Slovenská akademie věd, Slovenská republika
Vysoké učení technické v Brně, Česká republika

## Slide 2
Motivace
Existuje způsob vyjádření součinitelů asymptotického rozvoje před čelem trhliny ve flexoelektrickém materiálu pomocí součinitelů intenzity napětí zavedených v lineární elastické lomové mechanice?
Jestliže ANO (bude líp?), o jaký způsob a metodu se jedná, jaká má omezení a výhody?
Co dál?
  Co je to flexoelektrický efekt?
  Co je to tzv. vnější a vnitřní asymptotické řešení pro trhlinu ve flexoelektrickém materiálu?
  Jak tato řešení propojit pomocí singulární perturbační metody (singular matched asymptotic expansion method)
  Numerické výsledky

## Slide 3
Flexoelektrické materiály
Gradienty deformace způsobují změnu symetrie krystalové mříže a následně polarizaci i v centrosymetrických krystalech (direct effect).
Flexoelektrický jev je důsledkem kombinace velkých gradientů deformace a elektrické polarizace v dielektrických materiálech.
Flexoelektrický jev je vlastnost materiálu závislá na rozměrech vnitřní struktury materiálu.

## Slide 4
Rovnice rovnováhy
Konstitutuvní vztahy
Boundary conditions
délkový parameter jako materiálová charakteristika
flexoelectrické parametry
napětí vyššího řádu
Flexoelektrické materiály

## Slide 5
classical elasticity
flexo
nonlocal
local
Flexoelektrické materiály

## Slide 6
The outer and inner asymptotic solution in the flexoelectric solid
FEM study: ,
inner solution
outer solution
flexo FEM: Sládek & Sládek et. al., International Journal of Solids and Structures, 2021
SGET FEM: Kotoul et . al., Fatigue & Fracture of Engineering Materials & Structures, 2020

## Slide 7
, , , , , , ,
symmetry
isolated and traction free crack faces
INPUT
4th-order differential equations
, ,
, ,
OUTPUT
crack
outer asymptotic
solution
inner asymptotic solution
Analytical solution:
Mao & Purohit, Journal of the Mechanics and Physics of Solids, 2015
The outer and inner asymptotic solution in the flexoelectric solid

## Slide 8
The outer and inner asymptotic solution in the flexoelectric solid
Outer solution:
Inner solution:
gauge

## Slide 9
The singular matched asymptotic expansion method
out
in
for
and for

## Slide 10
The singular matched asymptotic expansion method

## Slide 11
The singular matched asymptotic expansion method
Mao & Purohit, Journal of the Mechanics and Physics of Solids, 2015

## Slide 12
Numerical results
The influence of the flecoelectricity and Poisson ratio on the parameter
,

## Slide 13
Numerical results
The influence of the component on the inner asymptotic solution
, , , , 0.2

## Slide 14
Numerical results
The crack opening displacement
, ,

## Slide 15
Numerical results
The Cauchy stress in front of the crack tip
, ,

## Slide 16
Numerical results
The electric potential in front of the crack tip
, , ,

## Slide 17
The authors acknowledge the supports by the Slovak Science and Technology Assistance Agency registered under number APVV-18-0004, VEGA-2/0061/20
Thank you for your attention